SPECIFICATION SHEET No 7

| Substrate | Steel |
| --- | --- |
| Pre-Treatment | Vapour Degrease |
| Type of Powder | 1st Coat Zinc Rich Powder, 2nd Coat Nylon Modified Polyester Powder |
| Film Thickness | 120 microns |

Photograph of panel after 1000hrs salt spray test

Test Conditions

The results shown below are based on mechanical, fluid and chemical tests which have been carried out under laboratory conditions and are given for guidance only. Actual product performance will depend upon the circumstances under which the product is used. The design, shape and configuration of a product can have a huge bearing on the corrosion resistance.

Mechanical Tests

| Type of Test | Test Standard | Result |
| --- | --- | --- |
| Salt Spray | ASTM B-117 -73, BS 3900 Part F4 | 1000hrs plus |
| Cross Hatch | 2mm Crosshatch BSN ISO 2409 | Pass |
| Impact | ISO 6272, DIN 55669, BS 3900 E13 | Pass |
| Flexibility | ISO6860 (Conical Mandrel) | Pass |
| Pencil Hardness | ISO 15184: 1998 | 3H |